Copyright 2007 by The American Institute of Architects (AIA)	5/07 (R 02/10)

1/09:  Lifebridge master version.

7/10:  MasterSpec updates incorporated.

SECTION 09671 - RESINOUS FLOORING

This Section has been revised to serve as the master specification for Lifebridge Health projects.

This Section specifies resinous flooring systems applied as self-leveling slurries.  These systems may be used for patient toilet/shower rooms with European showers for better slip resistance.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

GENERAL

RELATED DOCUMENTS

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

SUMMARY

Section Includes:

Resinous flooring systems.

ACTION SUBMITTALS

Product Data:  For each type of product indicated.  Include manufacturer's technical data, application instructions, and recommendations for each resinous flooring component required.

Samples for Initial Selection:  For each type of exposed finish required.

INFORMATIONAL SUBMITTALS

Installer Certificates:  Signed by manufacturer certifying that installers comply with specified requirements.

Material Certificates:  For each resinous flooring component, from manufacturer.

Material Test Reports:  For each resinous flooring system.

CLOSEOUT SUBMITTALS

Maintenance Data:  For resinous flooring to include in maintenance manuals.

QUALITY ASSURANCE

Installer Qualifications:  Manufacturer's authorized representative who is trained and approved for installation of flooring systems required for this Project.

Engage an installer who is certified in writing by resinous flooring manufacturer as qualified to apply resinous flooring systems indicated.

Source Limitations:  Obtain primary resinous flooring materials, including primers, resins, hardening agents, grouting coats, and topcoats, from single source from single manufacturer.  Provide secondary materials, including patching and fill material, joint sealant, and repair materials, of type and from source recommended by manufacturer of primary materials.

Pre-installation Conference:  Conduct conference at Project site.

DELIVERY, STORAGE, AND HANDLING

Deliver materials in original packages and containers, with seals unbroken, bearing manufacturer's labels indicating brand name and directions for storage and mixing with other components.

PROJECT CONDITIONS

Environmental Limitations:  Comply with resinous flooring manufacturer's written instructions for substrate temperature, ambient temperature, moisture, ventilation, and other conditions affecting resinous flooring application.

Lighting:  Provide permanent lighting or, if permanent lighting is not in place, simulate permanent lighting conditions during resinous flooring application.

Close spaces to traffic during resinous flooring application and for not less than 24 hours after application unless manufacturer recommends a longer period.

PRODUCTS

MANUFACTURERS

Manufacturers:  Subject to compliance with requirements, provide:

Desco Coatings, Inc; Metallix Floor.

MATERIALS

Retain this article if low-emitting materials are required for LEED-NC or LEED-CI Credit IEQ 4.2.  Coordinate product selection in other Part 2 articles to be sure that products selected comply.

VOC Content of Resinous Flooring:  Provide resinous flooring systems, for use inside the weatherproofing system, that comply with the following limits for VOC content when calculated according to 40 CFR 59, Subpart D (EPA Method 24):

Resinous Flooring:  100 g/L.

RESINOUS FLOORING

Resinous Flooring:  Abrasion-, impact- and chemical-resistant, decorative-aggregate-filled, epoxy-resin-based, monolithic floor surfacing designed to produce a seamless floor and integral cove base.

System Characteristics:

Color and Pattern:  As selected by Architect from manufacturer's full range.

Wearing Surface:  Textured for slip resistance.

Overall System Thickness:  60-80 mils

Prime Coat:

Resin:  Epoxy with metallic additive

Formulation Description:  100 percent solids.

Application Method:  Self-leveling slurry.

Thickness of Coats:  10 – 15 mils.

Number of Coats:  One.

Body Coat:

Resin:  Epoxy with metallic additive

Formulation Description:  100 percent solids.

Application Method:  Self-leveling slurry.

Thickness of Coats:  50 – 60 mils.

Number of Coats:  Two.

Aggregates:  Metallic Additive

Topcoat:  Sealing or finish coats.

Resin:  Chemical Resistant Urethane.

Formulation Description:  High solids.

Type:  Clear.

Finish:  Gloss

Number of Coats:  One

ACCESSORIES

Primer:  Type recommended by manufacturer for substrate and body coats indicated.

Waterproofing Membrane:  Type recommended by manufacturer for substrate and primer and body coats indicated.

Patching and Fill Material:  Resinous product of or approved by resinous flooring manufacturer and recommended by manufacturer for application indicated.

Metal Cap for Integral Cove Base:  Square metal cap approved by flooring manufacturer.

EXECUTION

PREPARATION

General:  Prepare and clean substrates according to resinous flooring manufacturer's written instructions for substrate indicated.  Provide clean, dry substrate for resinous flooring application.

Concrete Substrates:  Provide sound concrete surfaces free of laitance, glaze, efflorescence, curing compounds, form-release agents, dust, dirt, grease, oil, and other contaminants incompatible with resinous flooring.

Roughen concrete substrates as follows:

Comply with ASTM C 811 requirements unless manufacturer's written instructions are more stringent.

Repair damaged and deteriorated concrete according to resinous flooring manufacturer's written instructions.

Verify that concrete substrates are dry and moisture-vapor emissions are within acceptable levels according to manufacturer's written instructions.

Perform anhydrous calcium chloride test, ASTM F 1869.  Proceed with application of resinous flooring only after substrates have maximum moisture-vapor-emission rate of 3 lb of water/1000 sq. ft. (1.36 kg of water/92.9 sq. m) of slab area in 24 hours.

Perform plastic sheet test, ASTM D 4263.  Proceed with application only after testing indicates absence of moisture in substrates.

Perform relative humidity test using in situ probes, ASTM F 2170.  Proceed with installation only after substrates have a maximum 75 percent relative humidity level measurement.

Alkalinity and Adhesion Testing:  Verify that concrete substrates have pH within acceptable range.  Perform tests recommended by manufacturer.  Proceed with application only after substrates pass testing.

Resinous Materials:  Mix components and prepare materials according to resinous flooring manufacturer's written instructions.

Use patching and fill material to fill holes and depressions in substrates according to manufacturer's written instructions.

Treat control joints and other nonmoving substrate cracks to prevent cracks from reflecting through resinous flooring according to manufacturer's written instructions.

APPLICATION

General:  Apply components of resinous flooring system according to manufacturer's written instructions to produce a uniform, monolithic wearing surface of thickness indicated.

Coordinate application of components to provide optimum adhesion of resinous flooring system to substrate, and optimum intercoat adhesion.

Cure resinous flooring components according to manufacturer's written instructions.  Prevent contamination during application and curing processes.

At substrate expansion and isolation joints, comply with resinous flooring manufacturer's written instructions.

Apply primer over prepared substrate at manufacturer's recommended spreading rate.

Integral Cove Base:  Apply cove base mix to wall surfaces before applying flooring.  Apply according to manufacturer's written instructions and details including those for taping, mixing, priming, troweling, sanding, and topcoating of cove base.  Round internal and external corners.

Integral Cove Base:  4 inches (100 mm) high.

Apply self-leveling slurry body coats in thickness indicated for flooring system.

Apply topcoats in number indicated for flooring system and at spreading rates recommended in writing by manufacturer.

PROTECTION

Protect resinous flooring from damage and wear during the remainder of construction period.  Use protective methods and materials, including temporary covering, recommended in writing by resinous flooring manufacturer.

END OF SECTION 09671